| Title | Describe concrete tests in a civil engineering laboratory |
| --- | --- |
| Level | 4 | Credits | 8 |

| Purpose | People credited with this unit standard are able to describe, in a civil engineering laboratory: concrete test methods, and the reporting requirements, meaning, and applicability of concrete test results. |
| --- | --- |

| Classification | Infrastructure Civil Engineering > Infrastructure Laboratory |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	Evidence presented for assessment against this unit standard must be consistent with safe working practices and be in accordance with applicable organisational and legislative requirements.

2	Applicable legislation, regulations, rules, standards and codes include but are not limited to: Health and Safety at Work Act 2015, Hazardous Substances and New Organisms Act 1996, and their associated regulations and subsequent amendments;

ISO/IEC 17025:2018 General requirements for the competence of testing and calibration laboratories, available from https://www.iso.org/store.html;

NZS 3112.1:1986 Methods of test for concrete - Tests relating to fresh concrete,

NZS 3112.2:1986  Methods of test for concrete - Tests relating to the determination of strength of concrete, NZS 3112.3:1986 Methods of test for concrete - Tests on hardened concrete other than for strength; NZS 3112.4:1986 Methods of test for concrete - Tests relating to grout, available from https://www.standards.govt.nz/.

3	Evidence is required for two tests on fresh concrete and two tests on hardened concrete.

Tests for fresh concrete may include but are not limited to – Yield, Air Content, Slump, Spread, Unit Mass.

Tests for hardened concrete may include but are not limited to – Compression Strength, Flexural Strength, Density, Moulding of Cylinders, Splitting Tensile.

4	Definitions

Describe refers to stating the individual components of the test sequentially in terms of the relevant test method and organisational requirements.  Components will vary between tests and include but are not limited to – the sample specifications, equipment requirements, environmental requirements, units of measurement, purpose, and scope of the test.  Describe does not include the explanation of results, the interaction between tests, or their scientific basis.

Organisational requirements refer to instructions to staff on policy and procedures which are formally documented or generally accepted at the worksite.  This may include legislation; industry standards and methods; national and international standards and methods; standard operating procedures; specifications; manuals; and manufacturer’s information.

Outcomes and performance criteria

Outcome 1

Describe concrete test methods in a civil engineering laboratory.

Performance criteria

1.1	The test method is described in terms of scope, sample requirements, equipment, processes involved, and results.

Range	may include but is not limited to – equipment, apparatus, samples, technique, calibration, environment.

1.2	The factors that can influence the outcomes of the test are described.

Range	may include but is not limited to – temperature, humidity, environment, condition of sample, size of sample.

1.3	The quality assurance of the test is described.

Range	may include but is not limited to – test method, recording requirements, checking.

Outcome 2

Describe the reporting requirements, meaning, and applicability of concrete test results in a civil engineering laboratory.

Performance criteria

2.1	The reporting requirements for test results are described.

Range	may include but is not limited to – equipment, apparatus, samples, technique, calibration, environment, rounding, remarks.

2.2	The meaning and applicability of test results are described

Range	may include but is not limited to – uncertainty of measurement, specification reliability, limitations.

| Planned review date | 31 December 2024 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 19 February 2015 | 31 December 2021 |
| Review | 2 | 23 January 2020 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0101 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact Connexis - Infrastructure Industry Training Organisation qualifications@connexis.org.nz if you wish to suggest changes to the content of this unit standard.