| Title | Demonstrate knowledge of stains used in furniture finishing operations |
| --- | --- |
| Level | 3 | Credits | 4 |

| Purpose | People credited with this unit standard are able to explain: the composition and use of stains in furniture finishing operations; the advantages, disadvantages, and end uses for furniture stains; and personal protection, safe handling and storage requirements for furniture stains. |
| --- | --- |

| Classification | Furniture > Furniture Operations |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	Assessment Information

This unit standard may be assessed against on-job or off-job.

All activities and performance criteria must be carried out in accordance with reference text.

2	Reference

Jackson, A and Day, D, (2nd ed.) (1999). Good Wood Finishes. London, England: Popular Woodworking Books, which is available at: http://www.amazon.com.

3	Legislation relevant to this unit standard includes the Hazardous Substances and New Organisms Act 1996 (HSNO).

4	Definition

SDS (Safety Data Sheets) are documents containing information on toxic substances used in the worksite.  It is a requirement of the Environmental Protection Authority that all worksites using toxic substances have SDSs.

Outcomes and performance criteria

Outcome 1

Explain the composition and use of stains in furniture finishing operations.

Performance criteria

  - Types of stain are explained in terms of their composition and use.

Range	water-based stain, solvent-based stain, oil-based stain.

1.2	Stained finishes that do not require protective coats are explained in terms of their composition and use.

Range	stained waxes, protective wood stains, varnish stains.

Outcome 2

Explain the advantages, disadvantages, and end uses for furniture stains.

Range	water-based stain, solvent-based stain, oil-based stain, acrylic stain.

Performance criteria

2.1	Advantages and disadvantages of furniture stains are explained.

Range	a minimum of three advantages and three disadvantages are explained.

2.2	End uses of furniture stains are explained.

Range	a minimum of three end uses are explained.

Outcome 3

Explain the personal protection, safe handling and storage requirements for furniture stains.

Range	water-based stain, solvent-based stain, oil-based stain, acrylic stain.

Performance criteria

  - The personal protection requirements for furniture stains are explained in accordance with the SDSs for furniture stains.

  - Safe handling of furniture stains is explained in accordance with the SDSs for furniture stains.

  - The storage requirements for furniture stains are explained in accordance with the SDSs for furniture stains.

| Planned review date | 31 December 2024 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 19 March 2015 | N/A |
| Review | 2 | 27 August 2020 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0173 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact Competenz qualifications@competenz.org.nz if you wish to suggest changes to the content of this unit standard.