| Title | Bleach kraft pulp in wood pulp manufacturing |
| --- | --- |
| Level | 4 | Credits | 30 |

| Purpose | People credited with this unit standard are able to: demonstrate knowledge of the kraft pulp bleaching process; operate the kraft pulp bleaching plant; and monitor and control the performance of the kraft pulp bleaching plant. |
| --- | --- |

| Classification | Wood Fibre Manufacturing > Pulp Making |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

- Legislation and references

Legislation, regulations and/or industry standards relevant to this unit standard include but are not limited to the:

- Hazardous Substances and New Organisms Act 1996;

- Health and Safety at Work Act 2015;

- Resource Management Act 1991;

- Health and Safety at Work (Major Hazard Facilities) Regulations 2016.

2	Definitions

Operating parameters refer to the boundary conditions in which the operations are carried out in kraft pulp bleaching process.

Operating procedures refer to the process(es) that are worked through, e.g. standard operating procedure (SOP) in kraft pulp bleaching process.

RCA refers to root cause analysis.

TCC refers to trouble cause correct.

Worksite documentation refers to organisation policies and procedures that are documented in memo, electronic, or manual format and available in the workplace, and are consistent with manufacturer’s requirements.  They may include but are not limited to – standard operating procedures, site specific procedures, site safety procedures, equipment operating procedures, quality assurance procedures, product quality specifications, references, approved codes of practice, housekeeping standards, environmental considerations, sustainability, on-site briefings, supervisor’s instructions, and procedures to comply with legislative and local body requirements relevant to the pulp making industry.

3	Assessment information

Evidence presented for assessment against this unit standard must be consistent with safe working practices and be in accordance with applicable service information, worksite documentation and legislative requirements.  This includes the knowledge and use of suitable tools and equipment.

Outcomes and performance criteria

Outcome 1

Demonstrate knowledge of the kraft pulp bleaching process.

Performance criteria

1.1	Purpose of the kraft pulp bleaching process is explained.

1.2	Bleaching action of kraft bleaching agents is explained.

1.3	Operating parameters and capability of the kraft pulp bleaching process are explained.

Range	operating parameters include but are not limited to – chemical strength, retention time, physical state of chemical and method of addition, pH, pulp temperature, consistency.

1.4	Normal and emergency procedures for handling hazardous chemicals used in pulp bleaching are described.

Range	chlorine dioxide, hypochlorite, sodium hydroxide, oxygen, hydrogen peroxide, sulphuric acid.

1.5	Hazards associated with the kraft pulp bleaching process are identified and actions to be taken to minimise, or eliminate the hazards are explained.

Range	hazards may include but are not limited to – chemical interaction, chemicals.

1.6	Environmental considerations applying to kraft pulp bleaching, spill recovery systems are described.

Range	environmental considerations may include but are not limited to – bleaching chemical leaks, fibre loss, contaminated filtrate.

1.7	Consequences of non-conformance with worksite operating procedures are described.

1.8	Roles and responsibilities of the kraft pulp bleaching process operator are explained.

Outcome 2

Operate the kraft pulp bleaching plant.

Performance criteria

2.1	Safe work practices associated with the operation of the kraft pulp bleaching process are demonstrated.

Range	practices may include but are not limited to – isolation and plant access procedures, lock-outs or tag-outs, emergency stops, machine guarding, wearing appropriate safety equipment.

2.2	Bleach plant is set up, started up, operated, and shut down.

  - Operating parameters are set and adjusted to enable production requirements to be achieved.

Range	operating parameters – flow rate, temperature, pressure, chemical to pulp ratios, consistency, chemical strengths, pH.

2.4	Grade changes are completed in bleach plant.

2.5	Essential care and housekeeping requirements are carried out.

Outcome 3

Monitor and control the performance of the kraft pulp bleaching plant.

Performance criteria

3.1	Performance of the kraft pulp bleaching plant is monitored and parameters are controlled in accordance with operating parameters.

Range	control parameters – temperature, pH, flows, strength, chemical to pulp ratio, consistency, stack emissions;

performance parameters – brightness, shives, dirt, residual chemical.

3.2	Operating and equipment faults and malfunctions are identified, and relevant corrective actions are taken.

Range	equipment faults and malfunctions – mechanical, electrical, hydraulic, pneumatic, instrumentation, chemical, distributed control system.

3.3	Relevant problem-solving techniques are used to assist with trouble shooting.

Range		problem solving techniques may include but not limited to – RCA, TCCs, 5 whys technique.

3.4	Brightness, pH, temperature, and consistency of output pulp are monitored to meet specified requirements.

3.5	Production rate is regulated in accordance with requirements.

3.6	Production, maintenance notifications, and quality records are explained and completed.

| Planned review date | 31 December 2028 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 22 February 1995 | 31 December 2024 |
| Revision | 2 | 27 January 1997 | 31 December 2024 |
| Review | 3 | 25 February 1999 | 31 December 2024 |
| Review | 4 | 18 December 2006 | 31 December 2024 |
| Review | 5 | 24 October 2014 | 31 December 2025 |
| Review | 6 | 30 November 2023 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0173 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact Hanga-Aro-Rau Manufacturing, Engineering and Logistics Workforce Development Council qualifications@hangaarorau.nz if you wish to suggest changes to the content of this unit standard.