| Title | Cold work holes in aeronautical aluminium alloys |
| --- | --- |
| Level | 4 | Credits | 4 |

| Purpose | People credited with this unit standard are able to: prepare to cold work holes in aeronautical aluminium alloys; cold work holes; and carry out task completion activities. |
| --- | --- |

| Classification | Aeronautical Engineering > Aircraft Structures |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	All tasks must be carried out in accordance with enterprise procedures.

2	Definition

Enterprise procedures – procedures used by the organisation carrying out the work and applicable to the tasks being carried out.  Examples are – standard operating procedures, safety procedures, equipment operating procedures, codes of practice, quality management practices and standards, procedures to comply with legislative and local body requirements.

3	Cold working of holes by prestressing is to prepare for fastener installation, using the split sleeve, sleeveless, high interference, low interference, or combination method.

Outcomes and performance criteria

Outcome 1

Prepare to cold work holes in aeronautical aluminium alloys.

Performance criteria

1.1	Task is determined by reviewing maintenance documentation and enterprise procedures.

1.2	Work area is prepared, and resources are obtained and checked for serviceability or status.

Range	may include but is not limited to – publications, tools, materials, heat treatment states, equipment, safety equipment.

1.3	Cold working equipment is calibrated to meet task requirements.

Outcome 2

Cold work holes.

Performance criteria

2.1	Hole is prepared for cold working.

Range	ream, de-burr.

2.2	Hole is cold worked.

2.3	Hole is inspected, and any defects located.

2.4	Any defects are rectified.

2.5	Inspections are obtained.

Outcome 3

Carry out task completion activities.

Performance criteria

3.1	Item is prepared for use, storage, or transit.

3.2	Completion activities specific to the task and work area are carried out.

Range	may include but are not limited to – tool control, cleanliness, tidiness, return of publications, preparation for next activity, return of aircraft and systems to normal.

3.3	Leftover items, parts, and materials are disposed of.

Range	may include but is not limited to – serviceable, unserviceable, surplus, waste, scrap, hazardous.

3.4	Documentation is completed.

| Planned review date | 31 December 2024 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 19 June 1995 | 31 December 2016 |
| Revision | 2 | 7 August 1997 | 31 December 2016 |
| Revision | 3 | 8 May 2001 | 31 December 2016 |
| Review | 4 | 26 March 2007 | 31 December 2016 |
| Review | 5 | 18 June 2014 | 31 December 2021 |
| Review | 6 | 26 March 2020 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0028 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact ServiceIQ qualifications@serviceiq.org.nz if you wish to suggest changes to the content of this unit standard.