| Title | Carry out aeronautical NDT inspections using liquid penetrant methods |
| --- | --- |
| Level | 4 | Credits | 10 |

| Purpose | People credited with this unit standard are able to: prepare aeronautical parts for NDT (non destructive testing) inspections using liquid penetrant methods; inspect aeronautical parts using liquid penetrant methods; and complete post-inspection tasks. |
| --- | --- |

| Classification | Aeronautical Engineering > Aeronautical Non Destructive Testing |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

| Prerequisites | Candidates must pass the following vision examinations: Near vision acuity Natural or corrected near-distance acuity in at least one eye to show that the applicant is able to: read a minimum of Jaeger Number 2 or equivalent type and size letter at a distance of not less than 30.5 cm (12 inches) on a standard Jaeger test chart; or perceive an Ortho-Rater minimum of 8 (or similar test pattern). Colour contrast differentiation Capable of distinguishing and differentiating contrast among colours used in the method. |
| --- | --- |

Guidance Information

- All tasks must be carried out in accordance with enterprise procedures.

- Definition

Enterprise procedures – procedures used by the organisation carrying out the work and applicable to the tasks being carried out.  Examples are – standard operating procedures, safety procedures, equipment operating procedures, codes of practice, quality management practices and standards, procedures to comply with legislative and local body requirements.

Outcomes and performance criteria

Outcome 1

Prepare aeronautical parts for NDT inspections using liquid penetrant methods.

Performance criteria

1.1	Task is determined by reviewing maintenance documentation and enterprise procedures.

1.2	Work area is prepared, and resources are obtained and checked for serviceability or status.

Range	may include but is not limited to – publications, materials, tools, equipment, safety equipment, environmental conditions established, immediate area secured.

1.3	Identification of aeronautical parts are matched with documentation by comparing serial and/or part numbers.

1.4	Aeronautical parts are prepared for inspection.

Range	clean surface finish.

1.5	Inspection equipment is set up.

Range	dark room, optical aids.

Outcome 2

Inspect aeronautical parts using liquid penetrant methods.

Performance criteria

2.1	Penetrant is applied, and dwell-time observed.

Range	brush, spray, dip, flow.

2.2	Penetrant is removed.

Range	water wash, solvent, hydrophilic, lipophilic.

2.3	Developer is applied, and dwell-time observed.

Range	powder, aqueous and/or non-aqueous wet, water soluble and/or suspendible.

2.4	Aeronautical parts are inspected.

Range	inspection equipment, standards, specifications, precision measuring equipment.

Outcome 3

Complete post-inspection tasks.

Performance criteria

3.1	Inspected aeronautical parts are prepared.

Range	may include but is not limited to – storage, transit, post-test clean, inhibit, blank, pack.

3.2	Resources are checked for serviceability and returned to service or storage.

Range	may include but is not limited to – tools, equipment, safety equipment, publications.

3.3	Leftover materials are disposed of.

Range	may include but is not limited to – serviceable, unserviceable, waste, hazardous.

3.4	Documentation is completed.

Range	may include but is not limited to – labels, work cards, logbooks.

3.5	Work environment is left in a state that enables the next task to begin.

| Planned review date | 31 December 2024 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 23 April 1996 | 31 December 2016 |
| Revision | 2 | 7 August 1997 | 31 December 2016 |
| Revision | 3 | 8 May 2001 | 31 December 2016 |
| Review | 4 | 20 June 2006 | 31 December 2016 |
| Review | 5 | 24 October 2014 | 31 December 2021 |
| Review | 6 | 26 March 2020 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0028 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact ServiceIQ qualifications@serviceiq.org.nz if you wish to suggest changes to the content of this unit standard.