| Title | Demonstrate knowledge of yarn specification and measurement |
| --- | --- |
| Level | 4 | Credits | 15 |

| Purpose | People credited with this unit standard are able to: describe yarn constructional properties; demonstrate knowledge of yarn count measurement and calculation; describe yarn twist measurement and calculation; describe yarn moisture content measurement and calculation; describe yarn strength measurement and calculation; describe yarn oil and fatty matter content measurement and calculation; demonstrate knowledge of yarn shade specification, assessment, and measurement; and describe yarn evenness specification and testing. |
| --- | --- |

| Classification | Textiles Manufacture > Core Yarn Processing |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	Definition

Workplace procedures refer to the procedures used by the organisation carrying out the work and applicable to the tasks being carried out.  Examples are – standard operating procedures, safety procedures, equipment operating procedures, codes of practice, quality management practices and standards, procedures to comply with legislative and local body requirements.

2	Assessment information

All activities and evidence must be in accordance with workplace procedures.

Outcomes and performance criteria

Outcome 1

Describe yarn constructional properties.

Performance criteria

1.1	Yarn properties that are commonly used to specify yarn construction are described in terms of their nature, method of specification and their effect on yarn processing and product performance.

Range	yarn count, yarn twist, yarn strength and elongation, moisture content, extractable matter content, shade, evenness, bulk, friction.

Outcome 2

Demonstrate knowledge of yarn count measurement and calculation.

Performance criteria

2.1	Yarn count system is explained.

Range	may include but is not limited to – tex, denier, metric, Yorkshire skeins, Worsted, Galashiels, Dewsbury, cotton;

evidence of one is required.

2.2	Count measurement is described in terms of methods used to assess absolute count and count variation.

Range	includes – equipment used, sample selection, test procedure, calculation of results, calculation of variance, interpretation of results;

methods may include – laboratory test using wrap reel, doff weight and length, cross-card test.

Outcome 3

Describe yarn twist measurement and calculation.

Performance criteria

3.1	Factors used to define or calculate yarn twist are described.

Range	twist level, twist direction, single twist, ply twist, twist take-up, twist on twist effect, twist against twist effect, twist factor, ply combinations.

3.2	Twist measurement is described in terms of methods used to assess twist level, direction, and variation.

Range	includes – equipment used, sample selection, test procedure, calculation of results, calculation of variance, interpretation of results;

methods may include – calculation from machine settings, laboratory measurement using parallel fibre or ply, laboratory measurement using extension-contraction.

Outcome 4

Describe yarn moisture content measurement and calculation.

Performance criteria

4.1	Factors used to define or calculate yarn regain are described.

Range	dry weight, conditioned weight, moisture content percentage, regain percentage.

4.2	Measurement methods used for yarn moisture content measurement are described.

Range	includes – equipment used, sample selection, test procedure, calculation of results, calculation of variance, interpretation of results;

methods – dry to constant weight, electronic measurement.

Outcome 5

Describe yarn strength measurement and calculation.

Performance criteria

5.1	Factors used to define or calculate yarn strength are described.

Range	strength, strength per count unit, strength variation, extension at break.

5.2	Yarn strength measurement methods are described.

Range	equipment used, sample selection, test procedure, calculation of results, calculation of variance, interpretation of results.

Outcome 6

Describe yarn oil and fatty matter content measurement and calculation.

Performance criteria

6.1	Factors used to define or calculate oil and fatty matter content are described.

Range	extractable matter percentage.

6.2	Measurement methods for yarn oil and fatty matter content measurement are described.

Range	includes – equipment used, sample selection, test procedure, calculation of results, calculation of variance, interpretation of results;

methods may include – rapid extraction, soxhlet extraction.

Outcome 7

Demonstrate knowledge of yarn shade specification, assessment, and measurement.

Performance criteria

7.1	Factors that influence the assessment and measurement of shade are defined and described in terms of their effect on assessment and measurement.

Range	light source, viewing conditions, preparation and storage of standards.

7.2	Methods used for assessment and measurement of yarn shade are described.

Range	includes – equipment used, sample selection, test procedure, interpretation of results;

methods – visual assessment, colour measurement.

Outcome 8

Describe yarn evenness specification and testing.

Performance criteria

8.1	Factors used to define or calculate yarn evenness are described.

Range	count variation, Uster evenness index.

8.2	Yarn evenness measurement methods are described.

Range	includes – equipment used, sample selection, test procedure, calculation of results, calculation of variance, interpretation of results;

methods – wrap board, analysis of count variation, Uster evenness tester.

| Planned review date | 31 December 2026 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 18 June 1995 | 31 December 2019 |
| Revision | 2 | 8 August 1997 | 31 December 2019 |
| Revision | 3 | 18 July 2000 | 31 December 2019 |
| Revision | 4 | 10 October 2001 | 31 December 2019 |
| Revision | 5 | 12 August 2004 | 31 December 2019 |
| Review | 6 | 23 April 2008 | 31 December 2019 |
| Review | 7 | 19 May 2016 | 31 December 2025 |
| Review | 8 | 24 March 2022 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0030 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact Hanga-Aro-Rau Manufacturing, Engineering and Logistics Workforce Development Council qualifications@hangaarorau.nz if you wish to suggest changes to the content of this unit standard.