| Title | Demonstrate knowledge of and construct fibrous plaster radiant heating panels in a factory |
| --- | --- |
| Level | 4 | Credits | 10 |

| Purpose | People credited with this unit standard are able to: describe methods used to construct fibrous plaster radiant heating panels in a factory; make element grid in a factory for fibrous plaster radiant heating panels; and cast fibrous plaster radiant heating panels and arrange for testing and tagging, in a factory. |
| --- | --- |

| Classification | Construction Trades > Fibrous Plaster |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	Definitions

Green panels means freshly cast panels of fibrous plaster that have yet to be dried.

Services means any electrical power system or other outlet for the reticulation of services to the panel.

Specifications refers to documented instructions (oral, written, graphic) and may include any of the following:  manufacturer’s specifications, recommendations or technical data sheets; material specifications; specifications from a specialist source such as an architect, designer, engineer or a supervisor; site or work specific requirements.

2	All work practices must comply with the following:

Health and Safety in Employment Act 1992 and Health and Safety in Employment Regulations 1995; Resource Management Act 1991; Building Act 2004; New Zealand Building Code.

3	Credit for this unit standard indicates compliance with industry practice.  Industry practice refers to the ability to demonstrate knowledge and skills that reflect the productivity, uniformity, finish quality and material economies currently accepted within industry.

Outcomes and performance criteria

Outcome 1

Describe methods used to construct fibrous plaster radiant heating panels in a factory.

Performance criteria

1.1	Method of making element grid is described in accordance with radiant heating panel design.

1.2	Method of preparing mould is described in accordance with factory requirements.

1.3	Method of casting panel is described in accordance with factory requirements.

1.4	Method of testing element grid for electrical continuity is described in accordance with factory requirements.

1.5	Method of curing and storing green radiant heating panels is described in accordance with factory requirements.

Outcome 2

Make element grid in a factory for fibrous plaster radiant heating panels.

Performance criteria

2.1	Framework for element grid is made in accordance with radiant heating panel design.

2.2	Specified wire for element grid is run on framework in accordance with factory requirements.

2.3	Element grid is tested for electrical continuity.

Outcome 3

Cast fibrous plaster radiant heating panels in a factory and arrange for testing and tagging.

Performance criteria

3.1	Moulds are prepared in accordance with factory requirements.

3.2	Plaster is mixed, panels are cast and reinforced, and element grid is placed and checked in accordance with manufacturer’s specifications and industry practice.

3.3	Green panels are dried and stored to factory requirements.

3.4	Testing and tagging of radiant heating panels by a registered electrician is arranged.

3.5	All operations are completed, workplace, tools and moulds are cleaned, and tools and moulds are stored in accordance with factory requirements.

This unit standard is expiring.  Assessment against the standard must take place by the last date for assessment set out below.

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 18 January 1996 | 31 December 2024 |
| Revision | 2 | 5 July 1999 | 31 December 2024 |
| Review | 3 | 29 August 2000 | 31 December 2024 |
| Revision | 4 | 18 May 2005 | 31 December 2024 |
| Review | 5 | 20 April 2006 | 31 December 2024 |
| Review | 6 | 25 January 2008 | 31 December 2024 |
| Review | 7 | 26 May 2022 | 31 December 2024 |

| Consent and Moderation Requirements (CMR) reference | 0048 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.