| Title | Demonstrate knowledge of and cast fibrous plaster decorative mouldings in a factory |
| --- | --- |
| Level | 4 | Credits | 8 |

| Purpose | People credited with this unit standard are able to describe methods used to cast, cure and store fibrous plaster decorative mouldings; and cast fibrous plaster decorative mouldings in a factory. |
| --- | --- |

| Classification | Construction Trades > Fibrous Plaster |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	Definitions

Green mouldings means freshly cast mouldings of fibrous plaster that have yet to be dried.

Specifications refers to documented instructions (oral, written, graphic) and may include any of the following:  manufacturer’s specifications, recommendations or technical data sheets; material specifications; specifications from a specialist source such as an architect, designer, engineer or a supervisor; site or work specific requirements.

2	Performance of the elements must meet work requirements of a commercial environment.  Work requirements are detailed in the Industry Productivity Guidelines which are available from the Building and Construction Industry Training Organisation, PO Box 2615, Wellington.

3	All work practices must comply with the following:

Health and Safety in Employment Act 1992 and Health and Safety in Employment Regulations 1995; Resource Management Act 1991; Building Act 2004; New Zealand Building Code.

4	Credit for this unit standard indicates compliance with industry practice.  Industry practice refers to the ability to demonstrate knowledge and skills that reflect the productivity, uniformity, finish quality and material economies currently accepted within industry.

Outcomes and performance criteria

Outcome 1

Describe methods used to cast, cure and store fibrous plaster decorative mouldings.

Performance criteria

1.1	Method of preparing moulds is described in accordance with factory requirements.

Range	plaster, flexible, fibreglass, timber.

1.2	Method of casting and reinforcing mouldings is described in accordance with factory requirements.

Range	wall niche, ceiling centre, ceiling dome, ring, archway, corbel, fireplace, rail batten, dado.

1.3	Method of curing and storing green decorative mouldings is described in accordance with factory requirements.

Range	wall niche, ceiling centre, ceiling dome, ring, archway, corbel, fireplace, rail batten, dado.

Outcome 2

Cast fibrous plaster decorative mouldings in a factory.

Range	ceiling centre, and two of – wall niche, ceiling dome, ring, archway, corbel, fireplace, rail batten, dado.

Performance criteria

2.1	Moulds are prepared in accordance with factory requirements.

2.2	Plaster is mixed, and mouldings are cast and reinforced in accordance with manufacturer’s specifications, and industry practice.

2.3	Green mouldings are dried and stored to factory requirements.

2.4	All operations are completed, workplace, tools and moulds are cleaned, and tools and moulds are stored in accordance with factory requirements.

This unit standard is expiring.  Assessment against the standard must take place by the last date for assessment set out below.

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 18 January 1996 | 31 December 2024 |
| Revision | 2 | 5 July 1999 | 31 December 2024 |
| Review | 3 | 29 August 2000 | 31 December 2024 |
| Revision | 4 | 18 May 2005 | 31 December 2024 |
| Review | 5 | 20 April 2006 | 31 December 2024 |
| Review | 6 | 25 January 2008 | 31 December 2024 |
| Review | 7 | 26 May 2022 | 31 December 2024 |

| Consent and Moderation Requirements (CMR) reference | 0048 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.