| Title | Demonstrate knowledge of physical characteristics of wood |
| --- | --- |
| Level | 2 | Credits | 5 |

| Purpose | People credited with this unit standard are able to demonstrate knowledge of: the structure of radiata pine; wood types and the factors that impact on end use; and wood as a raw material. |
| --- | --- |

| Classification | Wood Manufacturing - Generic Skills > Wood Manufacturing Foundation Skills |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	Definitions

Accepted industry practice refers to approved codes of practice and standardised procedures accepted by the wider wood manufacturing industry as examples of best practice.

Workplace procedures refer to documented policies and procedures set by the organisation carrying out the work, and to documented or other directions provided to staff, and applicable to the tasks being carried out.  They may include but are not limited to – standard operating procedures, site specific procedures, site safety procedures, equipment operating procedures, quality assurance procedures, product quality specifications, references, approved codes of practice, housekeeping standards, environmental considerations, on-site briefings, supervisor’s instructions, and procedures to comply with legislative and local body requirements relevant to the wood manufacturing sector.

- Assessment information

All activities and evidence must meet workplace procedures and accepted industry practice.

Outcomes and performance criteria

Outcome 1

Demonstrate knowledge of the structure of radiata pine.

Performance criteria

1.1	Differences between earlywood and latewood are explained.

Range	differences include – density, moisture content, time of formation.

1.2	Differences between heartwood and sapwood are explained.

Range	differences include – function, location.

1.3	Differences between corewood and outerwood found in radiata pine are explained.

Range	differences include – density, moisture content, time of formation, end use.

1.4	The location of spiral grain in the log is identified.

Outcome 2

Demonstrate knowledge of wood types and the factors that impact on end use.

Performance criteria

2.1	The differences in hardwoods and softwoods are identified.

Range	leaves or needles, fruit or cones, thin or thick cell walls, deciduous or evergreen, covered or naked seed, round or conical shape.

2.2	The effects of age, geographical location, and climatic conditions on density are compared.

2.3	The impact of density on end use is described.

Outcome 3

Demonstrate knowledge of wood as a raw material.

Performance criteria

3.1	The physical characteristics of wood as a raw material are described.

Range	characteristics include – variability, durability, appearance, versatility, thermal conductivity, sustainability.

3.2	The advantages of wood as a raw material are compared with metals, plastics, concrete, and fibre-based products.

| Planned review date | 31 December 2024 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 27 January 1994 | 31 December 2012 |
| Review | 2 | 24 October 1996 | 31 December 2012 |
| Review | 3 | 10 February 1999 | 31 December 2012 |
| Revision | 4 | 14 March 2000 | 31 December 2012 |
| Review | 5 | 18 December 2006 | 31 December 2012 |
| Review | 6 | 15 April 2011 | N/A |
| Review | 7 | 28 May 2020 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0013 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact Competenz qualifications@competenz.org.nz if you wish to suggest changes to the content of this unit standard.