| Title | Recondition engine cylinder heads |  |  |
| --- | --- | --- | --- |
| Level | 4 | Credits | 12 |

| Purpose | People credited with this unit standard are able to: prepare to recondition engine cylinder heads; and recondition engine cylinder heads. |
| --- | --- |

| Classification | Motor Industry > Engines |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	Evidence presented for assessment against this unit standard must be consistent with safe working practices and be in accordance with applicable service information, and company requirements and legislative requirements.  This includes the knowledge and use of suitable tools and equipment.

2	Legislation, regulations and/or industry standards relevant to this unit standard include but are not limited to the current version of the Health and Safety at Work Act 2015; and any subsequent amendments and replacements.

3	Definitions

Company requirements refer to instructions to staff on policy and procedures that are available in the workplace.  These requirements may include – company policies and procedures, work instructions, product quality specifications and legislative requirements.

Service information may include – technical information for a vehicle, machine, or product detailing operation; installation and servicing procedures; manufacturer instructions; technical terms and descriptions; and detailed illustrations.

4	Assessment against this standard must include cast iron and aluminium alloy cylinder heads from both petrol and diesel multi-cylinder engines.

5	It is recommended that individuals first hold credit for Unit 32322, Demonstrate knowledge of automotive cylinder head reconditing practices, before being assessed against this standard.

Outcomes and performance criteria

Outcome 1

Prepare to recondition engine cylinder heads.

Performance criteria

1.1	Engine cylinder heads are cleaned and decarbonised.

Range	may include – chemical cleaning bath, scraping, buffing, media blasting.

1.2	Engine cylinder heads are hardness tested.

1.3	Engine cylinder heads are crack tested or pressure tested.

Outcome 2

Recondition engine cylinder heads.

Performance criteria

2.1	Cylinder heads are repaired.

Range	may include – cracks, corrosion, threads, straightening, coolant components, rocker components, valve components, cylinder head surfaces;

evidence of four is required.

2.2	Cylinder heads are machined.

Range	rocker components, valve components, cylinder head.

2.3	Engine cylinder head is vacuum tested.

| Planned review date | 31 December 2025 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 25 September 1997 | 31 December 2023 |
| Review | 2 | 28 February 2001 | 31 December 2023 |
| Review | 3 | 25 January 2008 | 31 December 2023 |
| Review | 4 | 25 February 2021 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0014 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact MITO New Zealand Incorporated info@mito.org.nz if you wish to suggest changes to the content of this unit standard.