| Title | Demonstrate knowledge of the principles of wood drying |  |  |
| --- | --- | --- | --- |
| Level | 2 | Credits | 5 |

| Purpose | People credited with this unit standard are able to demonstrate knowledge of: reasons for drying wood and uses of wood that does not require drying; permeability and density in wood; moisture content (MC) and the movement of moisture in wood; and methods of drying wood. |
| --- | --- |

| Classification | Wood Manufacturing - Generic Skills > Wood Manufacturing Foundation Skills |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

| Prerequisites | Unit 736, Demonstrate knowledge of physical characteristics of wood; or demonstrate equivalent knowledge and skills. |
| --- | --- |

Guidance Information

1	Reference

AS/NZS 4787:2001 Timber – Assessment of drying quality.

2	Definitions

Accepted industry practice refers to approved codes of practice and standardised procedures accepted by the wider wood manufacturing industry as examples of best practice.

Workplace procedures refer to documented policies and procedures set by the organisation carrying out the work, and to documented or other directions provided to staff, and applicable to the tasks being carried out.  They may include but are not limited to – standard operating procedures, site specific procedures, site safety procedures, equipment operating procedures, quality assurance procedures, product quality specifications, references, approved codes of practice, housekeeping standards, environmental considerations, on-site briefings, supervisor’s instructions, and procedures to comply with legislative and local body requirements relevant to the wood manufacturing sector.

3	Assessment information

All activities and evidence must meet workplace procedures and accepted industry practice.

Outcomes and performance criteria

Outcome 1

Demonstrate knowledge of reasons for drying wood and uses of wood that does not require drying.

Performance criteria

1.1	The main reasons for wood drying are listed.

Range	evidence of two is required.

1.2	Uses of wood that do not require drying are identified.

Range	evidence of two is required.

Outcome 2

Demonstrate knowledge of permeability and density in wood.

Performance criteria

2.1	Permeability is defined in relation to wood.

2.2	Effects of permeability on wood drying and treatment processes are explained.

2.3	The effect of earlywood and/or latewood on permeability and density is explained for radiata pine.

Outcome 3

Demonstrate knowledge of moisture content (MC) and the movement of moisture in wood.

Performance criteria

3.1	The locations of water in wood are identified.

3.2	The MC of commercial species of wood is identified for heartwood and sapwood in the green condition.

Range	radiata pine, douglas fir, rimu, eucalyptus.

3.3	Shrinkage variation from Fibre Saturation Point (FSP) (30%) to 12% MC is defined for radiata pine.

Range	rates – radial, longitudinal, tangential, longitudinal compression wood, longitudinal core wood.

3.4	Distortion defects are identified.

Range	bow, crook or spring, cup, twist.

3.5	The relationships between shrinkage, FSP, Shrinkage Intersection Point (SIP), and Equilibrium Moisture Content (EMC) are explained.

3.6	Shrinkage rates in radiata pine are identified, compared, and used to calculate shrinkage for different wood types.

Range	rates – radial, longitudinal, tangential, longitudinal compression wood, longitudinal core wood.

3.7	Factors affecting variation of EMC are explained.

Range	season, climate, location of product use, species, surface coating.

3.8	Suitable wood MC for different end uses for domestic and major export markets are identified.

Range	evidence of two domestic end uses and one export market end use is required.

3.9	Timber packing for stability and product quality is explained.

Range		number of boards per packet, fillet and bearer placement, long and short lengths, flush ends, transport mode.

3.10	Problems associated with incorrect packet build are described.

Range		problems – stability, fillet positioning, dimensions, effect on further processes, final product quality.

Outcome 4

Demonstrate knowledge of methods of drying wood.

Performance criteria

4.1	Components of the drying atmosphere are identified, and the theory of air movement is described.

4.2	Drying methods in current use in New Zealand are listed.

Range	evidence of five methods is required.

4.3	Typical drying times of radiata pine of a specified thickness, in the drying methods in performance criterion 4.2, are listed.

4.4	The concept of drying variability is explained in terms of standard deviation, range, target MC.

| Planned review date | 31 December 2024 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 5 July 1993 | 31 December 2012 |
| Review | 2 | 24 October 1996 | 31 December 2012 |
| Review | 3 | 10 February 1999 | 31 December 2012 |
| Revision | 4 | 12 December 2000 | 31 December 2012 |
| Review | 5 | 18 December 2006 | 31 December 2012 |
| Rollover and Revision | 6 | 15 April 2011 | 31 December 2015 |
| Review | 7 | 20 March 2014 | N/A |
| Review | 8 | 28 May 2020 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0013 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact Competenz qualifications@competenz.org.nz if you wish to suggest changes to the content of this unit standard.