| Title | Check and joint rebated fibre cement claddings with a proprietary plaster coating on site |
| --- | --- |
| Level | 4 | Credits | 20 |

| Purpose | People credited with this unit standard are able to: check fibre cement cladding on site is fit for purpose for jointing; describe remedial work as required to allow the jointing of fibre cement cladding; mask and protect adjoining surfaces to fibre cement cladding; prepare and complete the surface, joinery, junctions, transitions, and penetrations in the fibre cement cladding; mix and condition jointing compounds and describe specific storage conditions; and apply jointing compounds and reinforcement, and determine curing and protection requirements. |
| --- | --- |

| Classification | Construction Trades > Proprietary Plaster Cladding Systems |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	Definitions

Fibre cement cladding refers to the rebated fibre cement board or sheet that has in this instance been verified as a suitable cladding that can be jointed with a Proprietary Plaster coating.

On site refers to a wide range of building and construction environments within which the Proprietary Plaster Cladding Systems trade skills are applied.

Specifications refers to documented instructions (oral, written, graphic) and may include any of the following:  manufacturer’s specifications, recommendations or technical data sheets; material specifications; specifications from a specialist source such as an architect, designer, engineer or a supervisor; site or work specific requirements.

2	Legislation, regulations, codes and standards relevant to this unit standard include:

Health and Safety in Employment Act 1992;

Health and Safety in Employment Regulations 1995;

Resource Management Act 1991;

Hazardous Substances and New Organisms Act 1996; Building Act 2004;

New Zealand Standards, NZS 4218:2004 Energy efficiency – Small building envelope and NZS 3604:1999 Timber Framed Buildings, available from Standards NZ (http://www.standards.co.nz);

New Zealand Building Code;

Territorial Authorities’ building regulations.

3	Credit for this unit standard indicates compliance with industry practice.  Industry practice refers to the ability to demonstrate knowledge and skills that reflect the productivity, uniformity, finish quality and material economies currently accepted within industry.

Outcomes and performance criteria

Outcome 1

Check fibre cement cladding on site is fit for purpose for jointing.

Performance criteria

1.1	Cladding condition is checked on site as suitable for jointing in accordance with the manufacturer’s specifications.

Range	clean, dry, dust free, flat, correct thickness, rebated, neatly fitting.

1.2	Construction details are checked for compliance with the manufacturer’s specifications and working drawings.

Range	fixings, penetrations, flashings, control joints, interstorey joints, cavity details, ground clearance, fascia clearance.

Outcome 2

Describe remedial work as required to allow the jointing of fibre cement cladding.

Performance criteria

2.1	Actions required in the event that jointing of the fibre cement board cannot be undertaken in accordance with working drawings, specifications and manufacturer’s instructions, are described.

Range	three of – builder, designer, developer, owner, supplier, manufacturer, subcontractor.

Outcome 3

Mask and protect adjoining surfaces to fibre cement cladding.

Performance criteria

3.1	Masking products are identified and their application and purposes are described in terms of meeting the job requirements.

Range	PVC tape, paper tape, cloth tape, masking paper, plastic sheet, tape primer.

3.2	Types of masking equipment are identified and their uses are described in terms of meeting the job requirements.

Range	masking machines, tape dispensers.

3.3	Adjoining surfaces are masked in accordance with manufacturer’s specifications and work by other trades is protected in accordance with the job requirements.

Outcome 4

Prepare and complete the surface, joinery, junctions, transitions, and penetrations in the fibre cement cladding.

Performance criteria

4.1	The placement and fixing of PVC beads and proprietary flashings is determined and completed in accordance with jointing compound manufacturer’s specifications and job requirements.

Range	five of – base beads, angle beads, construction beads, joinery beads and flashings, parapet flashings, saddle flashings, control joints.

4.2	The surface preparation of the beads and flashings is determined and completed in accordance with the jointing compound manufacturer’s specifications and job requirements.

Range	cleaning, priming, stopping, joint rebate.

4.3	The preparation of the fibre cement cladding surface is determined and completed in accordance with jointing compound manufacturer’s specifications and job requirements.

Range	dryness, cleanliness, flatness, thickness, neatly fitting, surface preparation requirements, joint recessing.

4.4	The placement, size, and quality of flexible bead sealant is determined and applied in accordance with both the fibre cement and sealant manufacturers’ specifications and job requirements.

Outcome 5

Mix and condition jointing compounds and describe specific storage conditions.

Performance criteria

5.1	Measuring and mixing of selected proprietary jointing compounds are described and completed in accordance with compound manufacturers’ specifications and job requirements.

Range	six of – correct sequence of compounds, mixing instructions, weights, volumes, suitable container, drill mixers, water content, personal protection, proprietary additives.

5.2	Storage and care of mixed jointing compounds are described in accordance with manufacturers’ specifications.

Range	pot life, retempering, temperature, covering, contamination, disposal.

Outcome 6

Apply jointing compounds and reinforcement, and determine curing and protection requirements.

Performance criteria

6.1	Jointing compounds are applied to the fibre cement cladding in accordance with compound manufacturer’s specifications and job requirements.

Range	trowel, broadknife.

6.2	Joint reinforcement mesh tape is selected, cut and placed in accordance with compound manufacturer’s specifications and job requirements.

6.3	Curing and protection requirements for jointing compounds are determined in accordance with the material used, time of application, jointing compound, manufacturer’s specifications, weather conditions, and the working environment.

Range	three of – shade, weather protection, overcoat times, temperature, protection from site damage.

| Replacement information | This unit standard replaced unit standard 17506. |
| --- | --- |

This unit standard is expiring.  Assessment against the standard must take place by the last date for assessment set out below.

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 24 January 2006 | 31 December 2024 |
| Review | 2 | 26 January 2007 | 31 December 2024 |
| Review | 3 | 30 June 2022 | 31 December 2024 |

| Consent and Moderation Requirements (CMR) reference | 0048 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.