| Title | Apply nickel-cadmium to aeronautical components |  |  |
| --- | --- | --- | --- |
| Level | 4 | Credits | 10 |

| Purpose | People credited with this unit standard are able to: prepare to electroplate aeronautical components; carry out electro-chemical deposition of a nickel-cadmium infused coating; perform post-plate treatment; and complete the electroplating task. They are also able to operate, be in full control, and take responsibility for the process. |
| --- | --- |

| Classification | Aeronautical Engineering > Aeronautical Electroplating |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

- All tasks must be carried out in accordance with enterprise procedures.

- Definition

Enterprise procedures – procedures used by the organisation carrying out the work and applicable to the tasks being carried out.  Examples are – standard operating procedures, safety procedures, equipment operating procedures, codes of practice, quality management practices and standards, procedures to comply with legislative and local body requirements.

3	Acts, regulations, and bylaws regarding the handling of toxic material and waste must be complied with during assessment against this standard.

4	This unit standard applies to the electro-chemical deposition of a nickel-cadmium infused coating.

5	Operating parameters may include treatment times and currents, pH, temperature, anode condition, high temperature diffusion and inspection.

Outcomes and performance criteria

Outcome 1

Prepare to electroplate aeronautical components.

Performance criteria

1.1	Task is determined by reviewing maintenance documentation and enterprise procedures.

1.2	Component identity is confirmed with documentation.

1.3	Work area is prepared and checked.

Range	may include but is not limited to – materials, equipment, safety equipment, environmental conditions established.

1.4	Solution parameters are analysed to ensure process tolerances are met.

1.5	Pre-plate treatment is carried out.

Range	may include but is not limited to – non-destructive testing, stress relief of part having hardness of Rockwell C40 or above.

1.6	Component is prepared.

Range	may include but is not limited to – corrosion removal, jigging, masking.

Outcome 2

Carry out electro-chemical deposition of a nickel-cadmium infused coating.

Performance criteria

2.1	Solution is hard worked using a dummy cathode.

2.2	Component is chemically cleaned in accordance with enterprise procedures.

Range	may include but is not limited to – alkaline clean; anodic or periodic reverse cycle; acid etch.

2.3	Nickel is applied.

Range	may include but is not limited to – moving cathode bar; deposit thickness 0.0002-0.0004 inch.

2.4	Nickel deposit is visually inspected.

2.5	Cadmium is applied.

Range	deposit thickness 0.0001-0.0002 inch.

Outcome 3

Perform post-plate treatment.

Performance criteria

- 3.1	Conversion coating is applied.

3.2	Deposit is visually inspected.

3.3	Contact points are protected.

Range	heat resistant paint.

3.4	Coating is diffused by baking.

3.5	Diffused coating is visually inspected.

Outcome 4

Complete the electroplating task.

Performance criteria

4.1	Component is prepared for use, storage, or transit.

Range	may include but is not limited to – inhibiting, packing.

4.2	Resources are checked for serviceability and returned to service or storage.

Range	may include but is not limited to – tools, equipment, safety equipment.

4.3	Leftover parts and materials are disposed of.

Range	may include but is not limited to – serviceable, unserviceable, surplus, waste, scrap, hazardous.

4.4	Documentation is completed.

Range	may include but is not limited to – labels, work cards, release notes, certification.

4.5	Work area is left in a state that enables the next task to begin.

| Planned review date | 31 December 2027 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 26 March 2007 | 31 December 2016 |
| Review | 2 | 24 October 2014 | 31 December 2021 |
| Review | 3 | 26 March 2020 | N/A |
| Rollover and Revision | 4 | 26 April 2024 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0028 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact Ringa Hora Services Workforce Development Council qualifications@ringahora.nz if you wish to suggest changes to the content of this unit standard.