| Title | Apply metals to conductive aeronautical substrates using the selective (brush) plating process |  |  |
| --- | --- | --- | --- |
| Level | 4 | Credits | 10 |

| Purpose | People credited with this unit standard are able to: prepare to apply metals to aeronautical components; carry out electro-chemical deposition of metal to conductive aeronautical substrates; complete post-plate component inspection; and complete the plating process task. |
| --- | --- |

| Classification | Aeronautical Engineering > Aeronautical Electroplating |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

- All tasks must be carried out in accordance with enterprise procedures.

- Definition

Enterprise procedures – procedures used by the organisation carrying out the work and applicable to the tasks being carried out.  Examples are – standard operating procedures, safety procedures, equipment operating procedures, codes of practice, quality management practices and standards, procedures to comply with legislative and local body requirements.

3	Acts, regulations, and bylaws regarding the handling of toxic material and waste must be complied with during assessment against this standard.

4	If required, applicable electro-chemical deposition procedures can be found in US Air Force MIL-STD-865, Selective Brush Plating, Electro-Deposition.

5	This unit standard may apply to the electro-chemical deposition of a range of metals and alloys, which may include – babbitt, cadmium, cobalt, copper, iron, nickel, nickel-cobalt, nickel-tungsten, palladium platinum, rhodium, tin, zinc, silver, and gold.

6	Processing may be manual, semi or fully automatic;

operating parameters may include treatment times and currents, pH, temperature, anode condition, cleanliness of contacts, purity.

Outcomes and performance criteria

Outcome 1

Prepare to apply metals to aeronautical components.

Performance criteria

  - Task is determined by reviewing maintenance documentation and enterprise procedures.

  - Component identity is confirmed with documentation.

1.3	Work area is prepared and checked.

Range	may include but is not limited to – materials, equipment, safety equipment, environmental conditions established.

1.4	A process flowchart is designed.

Range	may include but is not limited to – technical data sheet, electro-clean, activate, pre-plate, metal or alloy.

1.5	Anode is prepared.

Range	may include but is not limited to – selection, design, manufacture, material, anode cover.

  - Ancillary equipment is prepared.

Range	may include but is not limited to – rectifier, solution pump, turning head, rotary tool, traversing arm, dial test indicator.

Outcome 2

Carry out electro-chemical deposition of metal to conductive aeronautical substrates.

Performance criteria

2.1	Component is masked.

Range	may include but is not limited to – tape, paint, lacquer, metallic foil, wax, plastic sheeting, fixtures.

  - Metal is applied to component using the selective (brush) plating process.

2.3	Equipment is monitored and adjusted.

Range	may include but is not limited to – solution pump, solution temperature, current density, voltage range, anode-cathode speed.

Outcome 3

Complete post-plate component inspection.

Performance criteria

3.1	Masking material is removed.

3.2	Quality control is carried out.

Range	may include but is not limited to – visual inspection, adhesion testing, accelerated corrosion testing.

3.3	Defects are rectified.

Outcome 4

Complete the plating process task.

Performance criteria

4.1	Component is prepared for use, storage, or transit.

Range	inhibiting, packing.

4.2	Solution amp-hr usage remaining is calculated and annotated.

4.3	Resources are checked for serviceability and returned to service or storage.

Range	may include but is not limited to – tools, equipment, safety equipment.

4.4	Leftover parts and materials are disposed of.

Range	may include but is not limited to – serviceable, unserviceable, surplus, waste, scrap, hazardous.

4.5	Documentation is completed.

Range	may include but is not limited to – labels, work cards, release notes, certification.

4.6	Work area is left in a state that enables the next task to begin.

| Planned review date | 31 December 2027 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 26 March 2007 | 31 December 2016 |
| Review | 2 | 24 October 2014 | 31 December 2021 |
| Review | 3 | 26 March 2020 | N/A |
| Rollover and Revision | 4 | 26 April 2024 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0028 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact Ringa Hora Services Workforce Development Council qualifications@ringahora.nz if you wish to suggest changes to the content of this unit standard.