| Title | Weld aluminium in downhand positions using the gas metal arc welding process |  |  |
| --- | --- | --- | --- |
| Level | 3 | Credits | 6 |

| Purpose | This unit standard is for people welding aluminium structures in downhand positions using the gas metal arc welding process (GMAW). People credited with this unit standard are able to: prepare to weld aluminium in the downhand positions using the GMAW process; weld aluminium in the downhand positions using the GMAW process; and inspect and repair aluminium GMAW welds. |
| --- | --- |

| Classification | Mechanical Engineering > Welding |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

| Prerequisites | Unit 33135, Demonstrate knowledge of safety and health while welding and thermal cutting, or demonstrate equivalent knowledge and skills. |
| --- | --- |

Guidance Information

1	Legislation and references

Legislation, regulations and/or industry standards relevant to this unit standard include but are not limited to the:

Health and Safety at Work Act 2015.

WorkSafe Good Practice Guide “Health and Safety in Welding”. Available at: https://www.worksafe.govt.nz/assets/dmsassets/WKS-13-Welding-GPG.pdf.

Weld Australia (formerly Welding Technology Institute of Australia (WTIA) Technical Note 7 – Health and Safety in Welding. Available at: Product Details  Weld Australia Member Portal.

Industry Standard - AS/NZS 1665: 2004, Welding of aluminium structures, or equivalent. Available at: www.standards.govt.nz.

Welder qualification Standards - AS/NZS 1665:2004 Welding of aluminium structures,

ISO 9606.2: 2004, Qualification testing of welders – Fusion welding – Part 2: Aluminium and aluminium alloys, or equivalent. Available at: www.standards.govt.nz.

ISO 6947:2019 Welding and allied processes – welding positions. Available at: www.standards.govt.nz.

Any new, amended or replacement Acts, regulations, standards, codes of practice, guidelines, or authority requirements or conditions affecting this unit standard will take precedence for assessment purposes.

2	Definitions

Accepted industry practice – approved codes of practice and standardised procedures accepted by the engineering industry as examples of best practice.

Aluminium – aluminium and weldable aluminium alloys.

Downhand positions – flat, and horizontal-vertical welding positions.

GMAW – Gas Metal Arc Welding; also referred to as Metal Inert Gas (MIG) Welding.

Industry standard – Category B of AS/NZS 1665:2004, or equivalent.

Manufacturer’s instructions – instructions provided by manufacturers of substances, equipment, and machinery.  These instructions may include details on safe and correct handling, use and storage of substances and/or details on substance properties.  Examples are labels on substance containers, product data sheets, and operator’s manuals.

Welding procedure – a work instruction providing all the necessary technical details for a specific welding application.

3	Assessment information

Evidence presented for assessment against this unit standard must be consistent with safe working practices and be in accordance with legislative requirements and workplace procedures and meet accepted industry practice. This includes the knowledge, use and maintenance of relevant tools and equipment.

Outcomes and performance criteria

Outcome 1

Prepare to weld aluminium in the downhand positions using the GMAW process.

Performance criteria

1.1	Equipment is selected to meet welding procedure requirements.

Range	power source rating and duty cycle, wire feed system and gun, shielding gas supply, welding cables, work clamp.

1.2	Equipment is assembled, set up, and maintained ready for use in accordance with manufacturer’s instructions.

Range	wire feed system, gun, shielding gas supply, welding cables, work clamp.

1.3	Aluminium components are prepared and assembled in accordance with welding procedure.

Range	edge preparation, cleaning, tack welding to correct alignment and preset.

1.4	Consumables are selected in accordance with welding procedure.

Range	electrodes are identified by specification and classification; shielding gases are identified by brand name and composition.

Outcome 2

Weld aluminium in the downhand positions using the GMAW process.

Range	six welds or test pieces:

material thickness 3.2 mm – 1G butt weld (temporary or permanent backing may be used) (ISO 6947 PA), 2F tee weld (ISO 6947 PB);

material thickness 6 mm and 10 mm – 1G butt weld (ISO 6947 PA), 2F tee weld (section to plate to include welding into a corner) (ISO 6947 PB).

Performance criteria

2.1	Workplace safety procedures are followed.

Range	examples are – use of personal protective equipment, checking of equipment for faults, use of fume extraction equipment, elimination of risk of fire or explosion, protection from arc radiation, protection from electrocution.

2.2	Welds are deposited on aluminium to industry standard and in accordance with welding procedure.

2.3	Component damage is minimised and distortion is controlled during welding and handling in accordance with accepted industry practice.

2.4	Welds are cleaned in accordance with accepted industry practice.

Outcome 3

Inspect and repair aluminium GMAW welds.

Performance criteria

3.1	Weld imperfections are identified by visual examination and workshop tests.

Range	examples of workshop tests are – nick break, fillet break-over, bend, macro examination;

two workshop tests are required for welds from Outcome 2.

3.2	Weld imperfections are evaluated using acceptance levels in industry standard.

3.3	A weld defect is repaired in accordance with welding procedure and to industry standard.

| Planned review date | 31 December 2027 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 30 November 1994 | 31 December 2022 |
| Revision | 2 | 14 April 1997 | 31 December 2022 |
| Revision | 3 | 5 January 1999 | 31 December 2022 |
| Review | 4 | 4 April 2001 | 31 December 2022 |
| Rollover and Revision | 5 | 20 April 2006 | 31 December 2022 |
| Review | 6 | 22 May 2009 | 31 December 2022 |
| Review | 7 | 20 July 2017 | 31 December 2025 |
| Review | 8 | 26 January 2023 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0013 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact Hanga-Aro-Rau Manufacturing, Engineering and Logistics Workforce Development Council qualifications@hangaarorau.nz if you wish to suggest changes to the content of this unit standard.