| Title | Weld aluminium in all positions using the gas metal arc welding process |  |  |
| --- | --- | --- | --- |
| Level | 4 | Credits | 10 |

| Purpose | This unit standard is for people welding aluminium structures in all positions using the gas metal arc welding process (GMAW). People credited with this unit standard are able to: prepare to weld aluminium in all positions using the GMAW process; weld aluminium in all positions using the GMAW process; and inspect and repair GMAW aluminium welds. |
| --- | --- |

| Classification | Mechanical Engineering > Welding |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	Legislation and references

Legislation, regulations and/or industry standards relevant to this unit standard include but are not limited to the:

Health and Safety at Work Act 2015.

WorkSafe Good Practice Guide “Health and Safety in Welding”. Available at: https://www.worksafe.govt.nz/assets/dmsassets/WKS-13-Welding-GPG.pdf.

Weld Australia (formerly Welding Technology Institute of Australia (WTIA) Technical Note 7 – Health and Safety in Welding. Available at: Product Details Weld Australia Member Portal.

Industry Standard - AS/NZS 1665:2004, Welding of aluminium structures, or equivalent.  Available at: www.standards.govt.nz.

Welder qualification Standards - AS/NZS 1665:2004, ISO 9606.2:2017 Qualification testing of welders Part 2: Aluminium and aluminium alloys, or equivalent. Available at: www.standards.govt.nz.

ISO 6947:2019, Welding and allied processes — Welding positions. Available at: www.standards.govt.nz.

Any new, amended or replacement Acts, regulations, standards, codes of practice, guidelines, or authority requirements or conditions affecting this unit standard will take precedence for assessment purposes.

2	Definitions

Accepted industry practice – approved codes of practice and standardised procedures accepted by the engineering industry as examples of best practice.

Aluminium – aluminium and weldable aluminium alloys.

GMAW – Gas Metal Arc Welding, also referred to as Metal Inert Gas (MIG) Welding.

Industry standard – Category B of AS/NZS 1665, or equivalent.

Manufacturer’s instructions – instructions provided by manufacturers of substances, equipment, and machinery.  These instructions may include details on safe and correct handling, use and storage of substances and/or details on substance properties.  Examples are labels on substance containers, product data sheets, and operator’s manuals.

Welding procedure specification (WPS) – written specification providing all the necessary technical details for a specific welding application meeting the requirements of the appropriate industry standard.

3	Assessment information

Evidence presented for assessment against this unit standard must be consistent with safe working practices and be in accordance with legislative requirements and workplace procedures and meet accepted industry practice.  This includes the knowledge, use and maintenance of relevant tools and equipment.

4	Recommended skills and knowledge

It is recommended that people seeking credit for this unit standard first hold credit for Unit 2675, Weld aluminium to industry standard in downhand positions using the gas metal arc welding process, or equivalent skills and knowledge.

Outcomes and performance criteria

Outcome 1

Prepare to weld aluminium in all positions using the GMAW process.

Performance criteria

1.1	Equipment is selected to meet WPS requirements.

Range	power source rating and duty cycle, wire feed system and gun, shielding gas supply, welding cables, work clamp.

1.2	Equipment is assembled, set up, and maintained ready for use in accordance with manufacturer’s instructions.

Range	wire feed system, gun, gun liner, nozzle and contact tip, shielding gas supply, welding cables, work clamp.

1.3	Aluminium is prepared and assembled in accordance with WPS.

Range	edge preparation, cleaning, tack welding to correct alignment, preset.

1.4	Consumables are selected in accordance with WPS.

Range	electrodes are identified by specification and classification; shielding gases are identified by brand name and composition.

Outcome 2

Weld aluminium in all positions using the GMAW process.

Range	5 welds;

material thickness – 5 to 10 mm;

welding positions – 2G, 3G, 4G, 3F, 4F (ISO 6947 PC, PF, PE, PF, PD).

Performance criteria

2.1	Workplace safety procedures are followed.

Range	use of personal protective equipment, checking of equipment for faults, use of fume extraction equipment, elimination of risk of fire or explosion, protection from arc radiation, protection from electrocution.

2.2	Measures to minimise welding distortion are applied in accordance with accepted industry practice.

Range	examples are – weld sequence, restraint, backstepping.

2.3	Welds are deposited on aluminium to industry standard and in accordance with WPS.

2.4	Welds are cleaned in accordance with accepted industry practice.

Outcome 3

Inspect and repair GMAW aluminium welds.

Performance criteria

3.1	Weld imperfections are identified by visual examination and workshop tests.

Range	examples of workshop tests – nick break, fillet break-over, bend, macro examination;

one workshop test is required for each weld from Outcome 2.

3.2	Weld imperfections are evaluated using acceptance levels in industry standard.

3.3	A weld defect is repaired in accordance with WPS and to industry standard.

Range	one of the following positions – 2G, 3G, 4G, 3F, 4F (ISO 6947 PC, PF, PE, PF, PD).

| Planned review date | 31 December 2027 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 30 November 1994 | 31 December 2022 |
| Revision | 2 | 14 April 1997 | 31 December 2022 |
| Revision | 3 | 5 January 1999 | 31 December 2022 |
| Review | 4 | 4 April 2001 | 31 December 2022 |
| Rollover and Revision | 5 | 20 April 2006 | 31 December 2022 |
| Review | 6 | 22 May 2009 | 31 December 2022 |
| Review | 7 | 20 July 2017 | 31 December 2025 |
| Review | 8 | 26 January 2023 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0013 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact Hanga-Aro-Rau Manufacturing, Engineering and Logistics Workforce Development Council qualifications@hangaarorau.nz if you wish to suggest changes to the content of this unit standard.