| Title | Service a simple mould for extrusion blow moulding |
| --- | --- |
| Level | 2 | Credits | 4 |

| Purpose | People credited with this unit standard are able to: identify the components of simple extrusion blow moulds for extrusion blow moulding; and perform servicing of a simple extrusion blow mould, blow pin, and extrusion pin and die. |
| --- | --- |

| Classification | Plastics Processing Technology > Extrusion Blow Moulding |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Explanatory notes

1	Legislation relevant to this unit standard includes but is not limited to the Health and Safety at Work Act 2015.

2	Definitions

Service includes inspection, cleaning, mould protection, and lubrication.  Other servicing requirements will depend on the organisation and may also include:

- refurbishing or replacing blow pin cut off sleeve

- polishing the extrusion pin and die

- requesting technical specialist assistance

- checking threads for damage if mould has back bolt holes.

Simple extrusion blow moulds may have the following features – central neck, single cavity, simple deflash, striker plates.  A simple mould also includes blow pin, extrusion pin and die, and stripper.

Workplace procedures – procedures used by the organisation carrying out the work and applicable to the tasks being carried out.  Examples are – standard operating procedures, site safety procedures, equipment operating procedures, codes of practice, quality management practices and standards, procedures to comply with legislative and local body requirements.

3	All evidence requirements must be performed in accordance with workplace procedures.

Outcomes and evidence requirements

Outcome 1

Identify the components of simple extrusion blow moulds for extrusion blow moulding.

Evidence requirements

1.1	Simple extrusion blow mould components are identified and their purpose described.

Outcome 2

Perform servicing of a simple extrusion blow mould, blow pin, and extrusion pin and die.

Evidence requirements

2.1	Mould is opened, and all moulding and mould contact surfaces, cavity surface finish, mould and blow pin cut-off, striker plate, and guide pins and bushes are inspected for damage and wear.  Results are recorded and reported.

2.2	Blow mould servicing is carried out.

2.3	Blow mould return to store procedures are performed.

Range	return to store procedures include – cooling water removal, cleaning, mould protection, lubrication.

| Planned review date | 31 December 2021 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 28 April 1993 | 31 December 2014 |
| Revision | 2 | 13 February 1997 | 31 December 2014 |
| Review | 3 | 23 January 1998 | 31 December 2014 |
| Review | 4 | 24 August 2006 | 31 December 2014 |
| Review | 5 | 21 March 2013 | 31 December 2019 |
| Review | 6 | 15 September 2016 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0013 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Please note

Providers must be granted consent to assess against standards (accredited) by NZQA, before they can report credits from assessment against unit standards or deliver courses of study leading to that assessment.

Industry Training Organisations must be granted consent to assess against standards by NZQA before they can register credits from assessment against unit standards.

Providers and Industry Training Organisations, which have been granted consent and which are assessing against unit standards must engage with the moderation system that applies to those standards.

Requirements for consent to assess and an outline of the moderation system that applies to this standard are outlined in the Consent and Moderation Requirements (CMRs).  The CMR also includes useful information about special requirements for organisations wishing to develop education and training programmes, such as minimum qualifications for tutors and assessors, and special resource requirements.

Comments on this unit standard

Please contact Competenz qualifications@competenz.org.nz if you wish to suggest changes to the content of this unit standard.