| Title | Peen aeronautical components |
| --- | --- |
| Level | 4 | Credits | 20 |

| Purpose | Persons credited with this unit standard are able to: prepare to peen aeronautical components; prepare a peening machine; peen aeronautical components; inspect peened aeronautical components; prepare aeronautical components; and carry out task completion activities. |
| --- | --- |

| Classification | Aeronautical Engineering > Aeronautical Machining |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	All tasks must be carried out in accordance with enterprise procedures.

2	Definition

Enterprise procedures – procedures used by the organisation carrying out the work and applicable to the tasks being carried out.  Examples are – standard operating procedures, safety procedures, equipment operating procedures, codes of practice, quality management practices and standards, procedures to comply with legislative and local body requirements.

3	May include – shot or bead peening.

Outcomes and performance criteria

Outcome 1

Prepare to peen aeronautical components.

Performance criteria

1.1	Component identity is confirmed with documentation by comparing serial and part numbers.

1.2	Task is established and documented.

1.3	Work area is prepared, and resources are obtained.

Range	may include but are not limited to – publications, materials, tooling, equipment, safety equipment, environmental conditions.

Outcome 2

Prepare a peening machine.

Performance criteria

2.1	Peening machine is prepared.

Range	condition checked, set up, adjusted, made safe to use.

2.2	Media is prepared.

Range	size, type, quality.

2.3	Almen test strip is prepared.

Range	air pressure, media type and weight, Almen strip type, time and distance.

2.4	Almen strip curvature is measured.

2.5	Machine is set for task requirement.

Range	air pressure, distance, time.

Outcome 3

Peen aeronautical components.

Performance criteria

3.1	Component is masked.

Range	holes, protected areas.

3.2	Component is peened.

Range	time, distance.

3.3	Masking is removed from component.

Outcome 4

Inspect peened aeronautical components.

Performance criteria

4.1	Component is measured and checked for conformity with specifications.

Range	dimensional and/or angular accuracy, profile, surface finish.

4.2	Any defects are reported, recorded, and rectified.

Outcome 5

Prepare aeronautical components.

Performance criteria

5.1	Component is prepared.

Range	may include but is not limited to – use, storage, transit, inhibiting, cleaning, packing.

5.2	Documentation is completed.

Outcome 6

Carry out task completion activities.

Performance criteria

6.1	Completion activities specific to the task and work area are carried out.

Range	may include but are not limited to – tool control, cleanliness, tidiness, return of publications, preparation for next activity, return of aircraft and systems to normal.

6.2	Leftover items, parts, and materials are disposed of.

Range	may include but is not limited to – serviceable, unserviceable, surplus, waste, scrap, hazardous.

| Planned review date | 31 December 2024 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 19 June 1995 | 31 December 2016 |
| Revision | 2 | 7 August 1997 | 31 December 2016 |
| Revision | 3 | 8 May 2001 | 31 December 2016 |
| Review | 4 | 26 March 2007 | 31 December 2016 |
| Review | 5 | 24 October 2014 | 31 December 2021 |
| Review | 6 | 26 March 2020 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0028 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact ServiceIQ qualifications@serviceiq.org.nz if you wish to suggest changes to the content of this unit standard.