| Title | Evaluate and interpret test indications found using optically aided NDT methods |
| --- | --- |
| Level | 5 | Credits | 12 |

| Purpose | People credited with this unit standard are able to: evaluate and interpret test indications found using optically aided NDT (non destructive testing) methods and prepare written NDT inspection reports; and direct testing personnel associated with the evaluation of the inspection results. |
| --- | --- |

| Classification | Aeronautical Engineering > Aeronautical Non Destructive Testing |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

- All tasks must be carried out in accordance with enterprise procedures.

- Definition

Enterprise procedures – procedures used by the organisation carrying out the work and applicable to the tasks being carried out.  Examples are – standard operating procedures, safety procedures, equipment operating procedures, codes of practice, quality management practices and standards, procedures to comply with legislative and local body requirements.

3	Optically aided inspections may include RVI (Remote Visual Inspection), RDVI (Remote Digital Visual Inspection).

Outcomes and performance criteria

Outcome 1

Evaluate and interpret test indications found using optically aided NDT methods and prepare written NDT inspection reports.

Performance criteria

1.1	Indications found during the inspection are evaluated and interpreted.

Range	confirmed, relevant, non-relevant, false.

1.2	Indistinct indications are confirmed using other NDT methods.

1.3	Inspection report is completed.

1.4	Test results are certified.

Outcome 2

Direct testing personnel associated with the evaluation of the inspection results.

Performance criteria

2.1	Personnel performing optically aided NDT inspections are directed.

| Planned review date | 31 December 2024 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 23 April 1996 | 31 December 2016 |
| Revision | 2 | 7 August 1997 | 31 December 2016 |
| Revision | 3 | 8 May 2001 | 31 December 2016 |
| Review | 4 | 20 June 2006 | 31 December 2016 |
| Review | 5 | 24 October 2014 | 31 December 2021 |
| Review | 6 | 26 March 2020 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0028 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact ServiceIQ qualifications@serviceiq.org.nz if you wish to suggest changes to the content of this unit standard.