| Title | Press formed wood furnish into composite panels |
| --- | --- |
| Level | 4 | Credits | 20 |

| Purpose | People credited with this unit standard are able to: explain fundamentals of composite panel pressing; operate and maintain composite panel press equipment; and monitor and control pre press, panel press equipment, and panel cooling and/or humidifying/conditioning systems for composite panel manufacture. |
| --- | --- |

| Classification | Wood Fibre Manufacturing > Composite Wood Panel Manufacturing |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Explanatory notes

1	Range:

Composite panels may include but are not limited to – medium density fibreboard (MDF), insulating board, particleboard, strandboard, fibre-faced strandboard, triboard;

evidence is required for one.

2	This unit standard is intended for work-based assessment.  While all evidence requirements must be met, some range statements within this unit standard are indicative and dependent on enterprise and worksite specific equipment, procedures, and practices.

3	The following apply to the performance of all outcomes of this unit standard:

a		All work practices must meet recognised codes of practice, documented worksite health and safety, and environmental procedures (where these exceed code), for personal, product and worksite health and safety.  They must also meet the obligations required under current legislation, including the Health and Safety in Employment Act 1992, the Resource Management Act 1991, and their subsequent amendments of these Acts.

b		All work practices must meet documented worksite quality management procedures.  This includes the recording (by electronic or non-electronic means) of activities, events, and decisions.

c		All communications must be made in accordance with worksite procedures for content, recipient, timing and method.

4	Definition

Worksite policies and procedures refer to documented policies, and to documented or other directions provided to staff.  These must conform to legislation, and include, but are not limited to, ways of managing health and safety, environmental considerations, quality, and production.  Examples include standard operating procedures, company health and safety plans, on-site briefings, and supervisor’s instructions.

Outcomes and evidence requirements

Outcome 1

Explain fundamentals of composite panel pressing in accordance with worksite policies and procedures.

Evidence requirements

1.1	The purpose of pressing operations in the composite panel manufacturing process is described.

Range		may include but is not limited to – pre pressing, pressing, post pressing;

evidence of a minimum of one is required.

1.2	The operating parameters and capability of presses are explained.

Range	may include but is not limited to – temperature, time in press, pressure and decompression cycles, moisture, profiles.

1.3	Operating components and process controls of presses are identified, and their purpose is explained.

Range	may include but is not limited to – frame, platens or plate, heat transfer system, transport system, thickness control system, hydraulic system, cooling system, fire prevention and detection system, vacuum system, lubrication system, simultaneous closing system, simultaneous opening system, distributed control systems, programmable logic controller, screens.

1.4	The purpose and stages of cycles used in the candidate’s own plant are described.

Range	cycles – pressure, temperature, time.

1.5	Pressing times used in the candidate’s own plant are explained in terms of required heat transfer for resin cure and/or lignin bonding in relation to panel thicknesses.

1.6	The need to reduce temperature and/or relieve stresses in composite panel boards immediately after pressing is explained in relation to the candidate’s own plant.

1.7	Hazards associated with composite panel pressing are identified and the role of protective equipment and safety features is explained.

Range	hazards may include but are not limited to – heat, dust, fumes, fire, explosions, hot oil, hot water;

safety features may include but are not limited to – personal protective equipment, hold cards, lockouts, stop buttons, guards, isolations, ventilation, fire protection.

1.8	The consequences of non-conformance with worksite operating procedures are described.

1.9	Reasons for trimming composite panels after pressing are explained.

Outcome 2

Operate and maintain composite panel press equipment in accordance with worksite policies and procedures.

Evidence requirements

2.1	Composite panel press equipment is set up, started up, operated, and shut down.

Range	set up may include but is not limited to – pressures, post-press equipment including trim saws and panel monitoring devices; installation of space bars for the required panel thickness; setting of decompression cycles, temperatures, speeds, press position; set up of the panel cooling and/or humidifying/conditioning equipment.

2.2	Operating faults and malfunctions are identified and corrective action is taken.

Range	may include but is not limited to – out-of-specification pressure, out-of-specification position, temperature variations, damage to platens and belts, delamination, blows, screens.

2.3	Equipment faults and malfunctions are identified and corrective action is taken.

Range	equipment faults and malfunctions may include but are not limited to – electrical, mechanical, hydraulic, pneumatic, instrumentation.

2.4	Pressed composite panels are processed.

Range	processed may include but is not limited to – panel cooling or humidifying/conditioning, quality checks, marking, stacking and transferring of panels to the next process.

2.5	Preventative maintenance and cleaning requirements are explained and applied.

2.6	Downgraded product is identified and communicated to downstream processing stages.

Outcome 3

Monitor and control pre-press, panel press equipment, and panel cooling and/or humidifying/conditioning systems for composite panel manufacture.

Evidence requirements

3.1	Monitoring and interpretation of feedback information, and adjustment of control parameters, enable process requirements, plant performance, and product quality to be maintained in accordance with worksite policies and procedures.

Range	may include but is not limited to – interpreting through panel density, panel thickness, panel flatness, panel internal temperature, cross panel density, blow/delamination detection.

3.2	Production rate is maintained in accordance with worksite policies and procedures.

3.3	Out-of-specification product is processed in accordance with worksite documentation.

3.4	Production, maintenance and quality records are completed in accordance with worksite policies and procedures.

| Planned review date | 31 December 2016 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 25 January 1995 | 31 December 2011 |
| Review | 2 | 24 November 1995 | 31 December 2011 |
| Revision | 3 | 12 February 1998 | 31 December 2011 |
| Review | 4 | 25 March 1999 | 31 December 2011 |
| Review | 5 | 29 March 2005 | 31 December 2011 |
| Review | 6 | 24 August 2006 | 31 December 2011 |
| Review | 7 | 25 January 2008 | 31 December 2012 |
| Review | 8 | 20 October 2011 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0173 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Please note

Providers must be granted consent to assess against standards (accredited) by NZQA, before they can report credits from assessment against unit standards or deliver courses of study leading to that assessment.

Industry Training Organisations must be granted consent to assess against standards by NZQA before they can register credits from assessment against unit standards.

Providers and Industry Training Organisations, which have been granted consent and which are assessing against unit standards must engage with the moderation system that applies to those standards.

Requirements for consent to assess and an outline of the moderation system that applies to this standard are outlined in the Consent and Moderation Requirements (CMR).  The CMR also includes useful information about special requirements for organisations wishing to develop education and training programmes, such as minimum qualifications for tutors and assessors, and special resource requirements.

Comments on this unit standard

Please contact the Competenz at info@competenz.org.nz if you wish to suggest changes to the content of this unit standard.