| Title | Adjust carpet tufter to produce carpet of specified pile weight |
| --- | --- |
| Level | 4 | Credits | 10 |

| Purpose | This unit standard is for people working in the carpet manufacturing industry. People credited with this unit standard are able to: demonstrate knowledge of carpet tufter adjustment; make tufter setting adjustments; and replace faulty gauge parts. |
| --- | --- |

| Classification | Textiles Manufacture > Carpet Manufacture |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

| Entry information |
| --- |
| Recommended skills and knowledge | Unit 7190, Tuft plain carpet. |

Explanatory notes

1	Legislation relevant to this unit standard includes but is not limited to the Health and Safety at Work Act 2015.

2	Definition

Workplace procedures – procedures used by the organisation carrying out the work and applicable to the tasks being carried out.  Examples are – standard operating procedures, site safety procedures, equipment operating procedures, codes of practice, quality management practices and standards, and procedures to comply with legislative and local body requirements.

3	Range

Plain and patterned tufters.

4	Assessment information

All evidence must be in accordance with workplace procedures.

Outcomes and evidence requirements

Outcome 1

Demonstrate knowledge of carpet tufter adjustment.

Evidence requirements

1.1	Tufter settings which may be changed to adjust pile weight are described in terms of their effect on the tufting process and product quality.

Range	stitch rate, yarn feed, tuft length.

1.2	Yarn properties are described in terms of their effect on tufting set-up, operating performance, and product quality.

Range	count, twist, strength, regain.

Outcome 2

Make tufter setting adjustments.

Evidence requirements

2.1	Adjustments are carried out.

2.2	Colour sequence at needles meets pattern specification.

2.3	Machine settings produce product to specification.

Range	stitch rate, yarn feed, tuft length, back stitch.

2.4	Carpet surface appearance meets product standard.

2.5	Samples are taken.

2.6	Sample test results are analysed, and machine settings calculated and adjusted to meet product specification.

2.7	Set-up records are maintained.

Outcome 3

Replace faulty gauge parts.

Range	needles, loopers, knives, reeds.

Evidence requirements

3.1	Gauge part changes are made.

3.2	Faulty gauge part is replaced according to machine requirement.

3.3	Replaced gauge part set and performs in accordance with workplace procedures.

| Planned review date | 31 December 2021 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 28 May 1996 | 31 December 2019 |
| Revision | 2 | 16 November 1998 | 31 December 2019 |
| Revision | 3 | 10 October 2001 | 31 December 2019 |
| Revision | 4 | 12 August 2004 | 31 December 2019 |
| Rollover and Revision | 5 | 26 March 2007 | 31 December 2019 |
| Rollover | 6 | 16 July 2010 | 31 December 2019 |
| Review | 7 | 19 May 2016 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0030 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Please note

Providers must be granted consent to assess against standards (accredited) by NZQA, before they can report credits from assessment against unit standards or deliver courses of study leading to that assessment.

Industry Training Organisations must be granted consent to assess against standards by NZQA before they can register credits from assessment against unit standards.

Providers and Industry Training Organisations, which have been granted consent and which are assessing against unit standards must engage with the moderation system that applies to those standards.

Requirements for consent to assess and an outline of the moderation system that applies to this standard are outlined in the Consent and Moderation Requirements (CMR).  The CMR also includes useful information about special requirements for organisations wishing to develop education and training programmes, such as minimum qualifications for tutors and assessors, and special resource requirements.

Comments on this unit standard

Please contact Competenz info@Competenz.org.nz if you wish to suggest changes to the content of this unit standard.