| Title | Carry out cathodic protection system monitoring in an energy and chemical plant |
| --- | --- |
| Level | 4 | Credits | 3 |

| Purpose | People credited with this unit standard are able to: assess, select, and operate cathodic protection system monitoring equipment; locate, interpret, and use documentation and reporting procedures for cathodic protection systems; and calculate and report results of testing cathodic protection systems; in an energy and chemical plant. |
| --- | --- |

| Classification | Energy and Chemical Plant > Monitoring of Energy and Chemical Plant |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

| Prerequisite | Unit 9575, Describe the purpose and application of cathodic protection in an energy and chemical plant, or demonstrate equivalent knowledge and skills. |
| --- | --- |

Guidance Information

1	Legislation and standards relevant to this unit standard include but are not limited to:

- Health and Safety at Work Act 2015;

- Health and Safety at Work (Hazardous Substances) Regulations 2017 (HSWA);

- Resource Management Act 1991;

- Standards relating to cathodic protection issued by:

National Association Corrosion Engineers (NACE), available at http://www.nace.org;

Standards Australia, available at http://www.saiglobal.com;

and any subsequent amendments.

- Definitions

Energy and chemical plant may be in – petrochemical, agri-nutrient, power generation, dairy processing, meat processing, and wood fibre manufacturing, or other plants that operate with a combination of high temperatures, pressures, steam and/or chemicals in gas, liquid or solid form.

Organisational requirements – documented policies and procedures.  These may include: equipment manufacturers’ procedures; plant procedures; suppliers’ instructions; site signage; codes of practice; company health and safety plans; on site briefings; and supervisor’s instructions.  This includes all regulatory and legislative obligations that apply to the plant.

Plant – the operational unit, equipment, and/or workplace at which the person is working.

Primary data refers to first analysis results.

- For the purposes of assessment:

- evidence for the practical components of this unit standard must be supplied from the workplace.

- evidence for all outcomes must be presented in accordance with organisational requirements.

Outcomes and performance criteria

Outcome 1

Assess, select, and operate cathodic protection system monitoring equipment in an energy and chemical plant.

Performance criteria

1.1	Assess the integrity of the cathodic protection system to determine the need to use cathodic protection system monitoring equipment.

1.2	Select cathodic protection system monitoring equipment relevant to site conditions.

1.3	Operate cathodic protection system monitoring equipment safely to determine the extent of maintenance required.

1.4	Identify and minimise any potential hazards from incorrect application and operation of cathodic protection system monitoring equipment.

Range	under protection, over protection.

Outcome 2

Locate, interpret, and use documentation and reporting procedures for cathodic protection systems in an energy and chemical plant.

Performance criteria

2.1	Locate and use specified documentation and standards for cathodic protection monitoring equipment.

Range	test certificates, certification, standards for safety, standards for in-service safety inspection and testing of equipment, identification tags, labels.

2.2	Locate and interpret general equipment documentation and information.

Range	manufacturer's information, equipment operating manuals, safety procedures, operating procedures, maintenance procedures.

2.3	Identify international cathodic protection standards and reporting criteria specific to the site.

Range	international standards – BSI British, Standards Australia, NACE.

Outcome 3

Calculate and report results of testing cathodic protection systems in an energy and chemical plant.

Performance criteria

3.1	Make any corrections to primary data in accordance with authorised procedures.

3.2	Calculate results from primary data.

3.3	Investigate and report any deviations from the expected range of results.

3.4	Compile a report including calculated results, analysis, and conclusions.

| Planned review date | 31 December 2025 |
| --- | --- |

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 6 February 1997 | 31 December 2018 |
| Revision | 2 | 3 August 2000 | 31 December 2018 |
| Review | 3 | 24 January 2002 | 31 December 2018 |
| Review | 4 | 20 February 2009 | 31 December 2018 |
| Rollover and Revision | 5 | 20 April 2017 | 31 December 2022 |
| Review | 6 | 27 February 2020 | N/A |

| Consent and Moderation Requirements (CMR) reference | 0079 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.

Comments on this unit standard

Please contact the Primary Industry Training Organisation standards@primaryito.ac.nz if you wish to suggest changes to the content of this unit standard.